# Luxalon® 84R façade system

## Part 1. 84R façade system general

  - 1.1 Introduction

Supply and fix Luxalon® 84R Façade System as manufactured by Hunter Douglas Architectural Products.

  - 1.2 Description of the system

The system will consist of linear rollformed aluminium panels with round edges, which can simply be clicked on the prongs of a stringer. The stringers are fixed on a non-Luxalon® sub-construction. To prevent contact corrosion by applying dissimilar metals, each fixing of the stringers to the sub-construction must be made through the Luxalon® washer set.

## Part 2. Product

________ m2 Luxalon® 84R Façade System consisting of:

  - 2.1 Panels

84R: size 84 x 16 mm manufactured from 0.6 mm aluminium. Panels to be manufactured from pre-painted, stove enamelled aluminium, corrosion resistant alloy EN-AW-3005 or equivalent (according to EN 1396 and EN13523).

Panels have a length of _________ mm (manufacturer availability 800-6000 mm, other lengths on request). Panels to be coupled in longitudinal direction by means of panel splices or by means of panel overlap. Curved panels with a radius of ______ mm. Panels have a length of ______ mm.

  - 2.2 Join Profiles

Flush join profiles, width 16 mm, manufactured from 0.35 mm aluminium Recessed join profiles, width 16 mm, manufactured from 0.65 mm aluminium Recessed join profiles, width 27 mm, manufactured from 0.65 mm aluminium

Join profiles to be manufactured from pre-painted, stove enamelled aluminium, corrosion resistant alloy EN-AW-3005 or equivalent (according to EN 1396 and ECCA). Join profiles have a standard length of 5000 mm. Join profiles to be

coupled in longitudinal direction by means of butting them together.

  - 2.3 Stringers

Rows of 0.95 mm thick aluminium rollformed stringers shall be installed at ________ centre to centre on a sub-construction consisting of a supporting steel or aluminium framing of sufficient strength and rigidity to provide

resistance to wind-pressure/suction. Stringers are provided with prongs to hold panels in a module of 146 mm (V2) or 157.7 mm (V3) or 90 mm (V4) or 100 mm (V5) or 111 mm (V6) or 116.6 mm (V8).

## Part 3. Additional specification

  - 3.1 profiles

Edge, trims drip sections, capping etc. made of stove enameled aluminium strip, with Luxacote® paint finish (± 30 micron).

  - 3.2 Coating

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® exterior 84R panels code no. ________ or a special colour will be made to match.

  - 3.3 Installation

All materials shall be installed in strict compliance with all local codes; ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown

on the drawings.