# LUXALON® CURVED PANEL 84R CEILING SPECIFICATION


PART 1: GENERAL

1.1 INTRODUCTION

# Supply and fix Luxalon® Curved Panel 84R Ceiling system as manufactured by Hunter Douglas Architectural Products.


1.2 DESCRIPTION OF THE SYSTEM

# The system will consist of curved panels fixed to an adjustable suspension system allowing all individual panels to be removed by hand. System featuring open joints between the panels that optionally can be closed with a recessed join profile.

# PART 2: PRODUCT

# _________m² Luxalon® Curved Panel 84R Ceiling featuring a 16mm joint, consisting of:

2.1 PANELS

Panels 84mm wide, 16mm deep, to be roll-formed from 0.5 mm thick stove enamelled aluminium strip, plain/perforated with/without non-woven acoustic textile.

JOIN PROFILES

Recessed join profiles, width 25mm, manufactured from 0.3mm aluminium.

Panels to be curved concave/convex with a fixed radius of approximately 325mm, featuring straight ends with a maximum flat distance of approximately 130 mm.

Panels to be curved concave/convex with a variable radius of minimum 1250mm, featuring no straight ends.

Curved panel ceiling optionally to be connected and proceeding in longitudinal direction with identical but straight panel ceiling.

Panels to be manufactured from pre-painted, stove enamelled, alloy HD 5050 or equivalent (according to EN 1396 and ECCA). All curved panels to have exact and identical radius and length measurements as indicated in drawing (manufacturer availability fixed radius 325mm or variable minimum radius 1250 mm and lengths 1000-6000 mm, on request > 6000 mm).

2.2 SUSPENSION

# Rows of 0.5 Fe/0.95 Alu roll-formed carriers shall be installed at _________ centre on centre (system maximum up to _________ mm) by means of rigid suspensions at a distance of _________, centre on centre. Carriers will be joined by means of carrier splices. Carriers to include integrated locking clips for locking the panels if desired.


PART 3: ADDITIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

# Custom solution, non Luxalon® materials.


3.2 PERFORATIONS

Manufacturer shall supply all 84R Carrier panels with the following perforation specifications:

  Ø 1.0 mm, Δ 2 mm, open area 23%

  Ø 2.0 mm, Δ 5 mm, open area 15%

Perforated panels to have a nominal plain border of 6 or 7 mm along the longitudinal panel direction to assure maximum flatness and product stability.


3.3 ACOUSTICS

# Manufacturer shall supply acoustic non-woven tissue, thickness 0.2 mm and factory applied inside the panels. Alternatively the installer can place individual, PE-wrapped mineral wool pads.


3.4 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® 84R panels code no. _________ or a special colour will be made to match.

The coating will consist of a tough and durable 2-layer polyester finish in nominal thickness of 20 microns, applied in a continuous coil-coating process ensuring uniform coating and absolute adhesion.


3.5 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.