## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon( 84R system as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of linear panels with round edges  fixed to an adjustable suspension system which allows for individual panels to be removed by hand. System to feature oen joints between the panels that can optionally be closed by clipping in flush join profiles.

## PART 2: PRODUCT

_________m2 Luxalon( 84R ceiling, featuring a 16 mm joint and consisting of:

  - PANELS

Panels, 84 mm wide, 16 mm deep, to be roll formed form 0.5 mm thick stove enamelled aluminium strip, plain/perforated with/without non-woven acoustic textile.

### JOIN PROFILES

- Flush join profiles, width 16mm, manufactured from 0.3 mm aluminium

- Flush join profiles with 3 x 7 mm ventilation holes, width 16 mm, manufactured fro 0.3 mm aluminium. Perforated flush joints profiles can be used in order to achieve a ventilating ceiling.

Panels to be manufactured from pre-painted, stove enamelled, alloy EN-AW-5050 or equivalent (according to EN 1396 and ECCA).

Panels have a length of ______mm (manufacturer availability 1000-6000 mm and

on request 250-1000 mm and > 6000 mm). Panels to be coupled in longitudinal direction by means of panel splices. Join profiles to be manufactured from pre-painted, stove enamelled aluminium, alloy EN-AW-5050 or  equivalent (according to En 1396 and ECCA). Joins allow for easy clipping into the open joint, without the use of additional tools.

  - SUSPENSION

Rows of 0.5 Fe/0.95 Alu roll formed carriers shall be installed at ______ centre on centre by means of adjustable suspensions at a distance of _________, centre on centre. Carriers will be joined by means of carrier splices. Carriers provided with prongs to hold panels in a standard module of 100mm (non-standard carriers are available to achieve a module between 93 and 150mm).

PART 3: ADDITIONAL SPECIFICATIONS

  - PERIMETER PROFILES

- Clip-on U-profile, 28.6x12.5 x20 mm, made of 0.35 thick aluminium

- Wall L-profile, 29.2x19.4 mm, made of 0.5 mm thick aluminium

- Wall L-profile, 45x18.5 mm, made of 0,8  mm thick steel or aluminium

- Wall W-profile, 45x21x21x18.5 mm, made of 0.8 mm thick steel or aluminium

  - PERFORATIONS

Manufacturer shall supply Luxalon( 84R panels with following perforation specifications:

- ( 1.0 mm, ( 2 mm with 23% open area

- ( 2.0 mm, ( 5 mm with 16%open area

Perforated panels to have a nominal plain border along the longitudinal panel

direction to assure a maximum flatness and product stability:

- 84R panel, 1 mm perforated to have a plain border of 7 mm

- 84R panel, 2 mm perforated to have a plain border of 6 mm

  - ACOUSTICS

Manufacturer shall supply acoustic non-woven tissue, thickness 0.2 mm  factory applied inside the panels. Alternatively the installer can place individual  PE wrapped mineral wool pads.

  - COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon 84R panels code no._________or a special colour will be made to match.

The coating will consist of a tough and durable polyester finish in nominal thickness of 20 microns, applied in a continuous coil-coating process ensuring uniform coating and absolute adhesion.

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.