## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon( Clip-In tile Ceiling System as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of bevelled edged tiles fixed to an adjustable suspension system which allows removable tiles to clip in place.

## PART 2: PRODUCT

2.1 TILES

________m2 Luxalon( Clip-In Tile Ceiling consisting of:

___x___tiles made of 0.5 mm steel or 0.6 mm aluminium

___x___swing-down tiles made of 0.6 mm steel

Two sides of each tile will be raised and pipped and stopped to ensure positive engagement into the spring tee yet allow for demounting of individual tiles. All tiles will be bevelled edged in bevel size 3 mm.

  - PRIMARY SUSPENSION

Rows of 0.5 mm galvanised steel common profiles shall be installed at 1200 mm centres by means of __mm high rod hangers or nonius hangers fixed to the upper structure at a maximum distance of 1250 mm centre to centre. Primary suspension profiles will be fixed at both ends to the wall to prevent upward movement.

## PART 3: ADDITIONAL SPECIFICATIONS

  - EDGE COVER PROFILES

- L-profile 25  x  25 mm made of 1.5 mm thick steel aluminium

- W-profile 25 x 25 x 25 x  25 mm made of 1.5  thick aluminium

- F-profile, 25 x 25 mm, made of 1.5 thick aluminium.

  - PERFORATIONS

Manufacturer shall supply tiles with perforation pattern no.____ with a nominal 10 mm plain border on all sides.

Perforations will have a ________diameter hole resulting in a ____% open area. Other borders on request.

  - ACOUSTICS

Manufacturer shall supply acoustic non-woven textile, thickness 0.2 mm glued into the tiles or black faced PE wrapped mineral wool thickness ___mm density___kg/m3 and of a size to completely fill the tile.

  - COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon( Tiles RAL code no._______or a special colour will be made to match.

The coating will consist of a tough and durable polyester powder coating finish in minimal thickness of 60 microns, electro statically applied into electro-galvanised steel, phosphates and chemically treated according to high industrial standards (DIN 1541/ TAIM standards).

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.

  - SUBSTITUTIONS

Ceiling installers wishing to submit proposals on systems other then the Luxalon® Tile Ceiling System shall, at least 10 days in advance of the bid date, submit to the architect complete descriptive information of the total system concept and performance data tests made as a system. In addition include a list of similar installations of the proposed substitution. If approval is made an addendum will be issued enumerating such approved system as herein set forth.