| Product | Hunter Douglas® Sliding Shutter Screen System |
| --- | --- |
| System | Sliding Shutter with screen fabric |
| Fabric | Enduris™ Glass Core screen fabric |
| Frame | Concealed aluminium frame |
| Vertical | aluminium extruded box profile 60x50 mm with gap for concealed screen fixing |
| Horizontal | aluminium extruded channel profile 60x42 mm with snap-in cover, edge for concealed screen fixing and sloped plane to reduce pollution |
| Sizes | Height______ Width______ (max. dimensions depending on wind loads) |
| Top rails | Aluminium extruded rectangular profile 40 x 48 mm |
| Bottom rails | Aluminium extruded T-profile 50 x 50 mm |
| Fabric openness | 3% open Heat and light transmittance properties vary per colour; data available on request |
| Fabric material | PVC-coated fibreglass fabric, thermofixated Twill Weave, 525 gr/m2 (Sergé 2165) |
| Fire resistance (screen fabric) | M1 (NF P92-503), Type B (BS 5867), B1 (DIN 4102), FR (NFPA 701), Classe 1 (UNI 9176-D) |
| Fabric colour | Choice of 34 fabrics offering 59 different screen colours |
| Screen fixing | Concealed fixing with stainless steel fastening materials in A2 (304) quality |
| Alloy extrusions | Al-Mg-Si 0.5 F22 (EN-AW 6060 T6/T66) |
| Finish aluminium | Natural anodised 20 microns (VOM1/A20/VB6) Custom colour anodised (limited range) 20 microns Polyester powder coated to RAL or other industry standard colour, thickness 60 microns, gloss ___% (standard gloss 70%) Polyester powder coated to RAL or other industry standard colour, thickness 90 microns, gloss ___% (standard gloss 70%) |
| Rail fixation | Rail fixed to façade or floor by means of aluminium brackets |
| Accessories | Hunter Douglas® top runners, bottom runners and end stop |
| Motorization | Optional: proprietary Hunter Douglas Sliding Shutter Drive system 1 / 2 / 3 / 4 shutters driven by one motor |
| Optional | automated control system |