| Product | : Hunter Douglas® Sun Louvre System 132S |
| --- | --- |
| System | : Fixed system, vertical applications |
| Shape | : Z-shaped panels with backrolled rounded edges |
| Panel section | 132S: 105.5 x 132 mm, thickness 0.6 mm |
| Panel length | : max. 6000 mm |
| Alloy | : EN-AW 3005 |
| Surface treatment | : Frontside: Luxacote® finish, 3 layer, 40 mµ, colours; see colour chart |
| Backside | : polyester coating, standard white |
| Panel fixing | : Panel bracket 132S extruded, anodised aluminium |
| Spacers | : 48, 63 and 88 mm extruded, anodised aluminium spacers for different panel modules |
| Panel modules 132S: | Spacer Module Shadow angle 88 mm 132 mm 0° 2x63 mm 171 mm 21° 2x88 mm 221 mm 42° |
| Support fixation | : Support fixed to façade by means of hot dip galvanised steel console, with extra aluminium top brace as an option |
| Support system | : Aluminium extruded supporting rail for panels and spacers |
| Rail support | : Railclamp with washer set |
| Fixing | : Clip system |
| Installation | : Spacers and panel brackets are sliding into support rail which is fixed with rail clamp to substructure (not Hunter Douglas® program) |